## CMP Seminar

Michigan State University

## Wei Lai

Chemical Engineering & Materials Science

Michigan State University

Rattling or Diffusing: atomic dynamics from combined computational and experimental studies

Various materials properties, e.g. structural, thermal, electrical, are strongly affected by atomic dynamics.  However, our understanding of atomic dynamics in complex multicomponent materials are often limited because the desired spatial (Å), temporal (ps), and chemical (element) resolutions are often difficult to achieve with a single probe.  In this talk, I will illustrate our combined computational and experimental efforts to study anomalous vibrational (rattling) and diffusive dynamics of two energy materials:  tetrahedrite thermoelectrics and lithium garnet oxide superionics, using computational (force-field and DFT base molecular dynamics simulation) and experimental probes (synchrotron diffraction, EXAFS, neutron total-scattering, quasi-elastic neutron scattering, etc).  Insight into the ratting dynamics of Cu in tetrahedrites and diffusive dynamics of Li in garnets will be presented and discussed.

Monday, September 25, 2017

4:10 p.m.

BPS 1400

Norman Birge & Ruby Ghosh - Host